## Slide 1
Towards Wearable Sensors for Wireless pH Monitoring in Sweat
Giusy Matzeu, Claudio Zuliani, Dermot Diamond
Clarity, Centre for Sensor Web Technology, Dublin City University, Ireland
Pittcon, 14/03/2012
1

## Slide 2
2

## Slide 3: Sensors for the Digital World
Analyte
Chemo/Bio Sensing
Wireless data transmission
4

## Slide 4: Sensors for the Digital World
IS-Membrane
Conducting Polymer
Carbon
Resist
Silver
PET Substrate
Cost
Reproducibility
Compatible with Wearable & Environmental Applications
5

## Slide 5: pH ISE – An Initial Design
Sensors and Actuators B, 2010, 146 , 19
2nd calibration after 3days in the conditioning solution
May we improve this limit working on SPE fabrication ?
6
1st calibration after overnight conditioning
Loss of linearity & offset change over time.
Notes: Membrane Composition:
● PVC 32.3% , o-NPOE 66.6%, KTpClPB 0.48%, H Ionophore II 0.66%
Dissolved in 3 ml of THF
Conditioning: Buffer 0.001 M di acido citrico, acido borico and Na2HPO4 a pH 4 overnight
Density of POT 2.75 mg/ml in 3 ml of chloroform.
30 ul of POT were drop cast on top of the electrodes

## Slide 6: “Initial” vs “New” SPE
7

## Slide 7
“Original” vs “New” SPE
Original SPE
0.3 < σ < 0.6
σ ≈ 1.6
8
New SPE

## Slide 8
pH ISEs – Silverless-SPE and Membrane Thickness
550 μm well allows a better reproducibility !
500 μm PMMA + 50 μm PSA as masking layer
175 μm PMMA + 50 μm PSA as masking layer
10
Carbon prints were masked used PSA and PMMA. PET substrate were laminated with PSA and PMMA after that tracks carbon was screen printed: Integration of ISE within microfluidic system

## Slide 9: pH ISEs – Performance over Time & Storage
Calibration repeated after 5 days storage in conditioning solution
11
Printing protocols, e.g., presence of Ag,, have a significant impact in sensor reproducibility over time !
Day 0
Day 5 (kept in conditioning solution)
Day 19 (kept in dry conditions)
Dry storage may preserve sensor functionality !

## Slide 10: Reference Electrodes based on Lipophilic Salts on SPE
U. Mattinen, J. Bobacka, A. Lewenstam, Electroanalysis 2009, 21, 1955.
SC=PEDOT
0.1 M KCl
1 mM KCl
1 mM NaCl
0.1 M NaCl
0.1 M KCl
Cl- ≈ 20 mV/decade
Possibility for RE where [Cl-] is constant
Need optimisation
SC=PEDOT
SC=POT
0.1 M KCl
1 mM KCl
1 mM NaCl
0.1 M NaCl
0.1 M KCl
13

## Slide 11: Mote Interface and Wireless Communication
• Mote 1
• Mote 2
• Mote 3
• 16Ch-Lawson Labs
Bias between motes and standard instrumentation < 0.3mV
Bias between motes < 0.1 mV
14

## Slide 12: Dual SPE – Integration of pH & RE on same substrate
The two carbon disks printed on the PET substrate will be modified to give a pH and a reference electrode
The substrate can also be laminated with PSA and PMMA for futher integration within microfluidics.
15
Work currently under progress to optimize sensor response !!

## Slide 13: Wearable pH Sensor –Concept
Mote Casing
Strap
Patch
Sensor + Microfluidic
16

## Slide 14: Wearable pH Sensor –Layers
Microfluidics
pH ISE & RE
Patch
Mote Casing
Mote
17

## Slide 15: Acknowledgements
Prof. Dermot Diamond
Dr. Fiachra Collins, postdoc
Javier Torres, Tyndall
Giusy Matzeu, PhD student
Dr. Salzitsa Anastasova, Dr. Aleksandar Radu,
Dr. Ulriika Mattinen,
Prof. Johan Bobacka
18

## Slide 16: CLARITY Centre & Ecosystem
SOCIAL/AGENCY COLLABORATORS
INDUSTRY COLLABORATORS
CSET CORE
16
SOCIAL/AGENCY COLLABORATORS
INDUSTRY COLLABORATORS
SOCIAL/AGENCY COLLABORATORS
INDUSTRY COLLABORATORS
19

## Slide 17: Thank You for Attention
20

## Slide 18: pH ISEs – Role of SPE Design
A comparison between 1° calibration for (Ag+C) SPE & C (Batch II) SPE
(Ag+C) SPE
C SPE
12