## Slide 1
Recent Progress in Disposable Ion-selective Sensors for Environmental Applications
Giusy Matzeu, Claudio Zuliani and Dermot Diamond
CIMTEC 2012,
Montecatini Terme

## Slide 2
1
Summary
Introduction
  Ion Selective Electrodes (ISEs)
Lead ISEs: Optimization for reproducibility
  POT
  PEDOT
New materials for the solid contact
  Gold Nanoparticles (GNPs)

## Slide 3
2
Introduction
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
Ion Selective Electrode (ISE) able to detect the analyte of interest
Analyte
Chemo/Bio
Sensing
Wireless Data Transmission
ISE integrated into a wireless device for in situ monitoring

## Slide 4
3
How to make an ISE
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
Screen Printing Technology
Cost
Reproducibility
OPTIMIZATION in terms of SOLID CONTACT
through Lead ISEs using different materials
Notes: Substrates can be adapted for the appropriate sensing strategy

## Slide 5
4
Solid Contact materials
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
The materials under analysis in terms of reproducibility:
  Poly(3-octylthiophene-2,5-diyl) (POT)
  Poly(3,4-ethylenedioxythiophene) (PEDOT)
  Gold nanoparticles soluble in water or
  methanol
Notes: investigation of materials to improve repro. of lead sensors

## Slide 6
5
POT
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
  POT was drop cast in different amounts
50 μm
50 μm
THICKNESS is changing
50 μm
Notes: aims
Optimization of a material and study of different materials
POT thickness

## Slide 7
6
POT
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
  Example of a calibration curve realized using POT like solid contact layer
SPE | Sensitivity (mV) | Baseline (mV)
1 | 48.15 | 339.3
2 | 46.36 | 339.7
3 | 43.16 | 343.9
4 | 44.43 | 333.7

## Slide 8
7
POT
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
How the performances of the Lead ISEs were affected in changing the amount of POT drop cast
● Standard deviation for the baseline of the ISEs
■ Standard deviation for the sensitivity of the ISEs

## Slide 9
8
PEDOT
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
  For PEDOT the performances are affected by the thickness and the redox state of the conducting polymer
50 μm
50 μm

## Slide 10
9
PEDOT
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
  Example of a calibration curve realized using PEDOT like solid contact layer
SPE | Sensitivity (mV) | Baseline (mV)
1 | 27.57 | 289.1
2 | 27.45 | 294
3 | 27.06 | 292.7
4 | 28.02 | 288.8

## Slide 11
10
PEDOT
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
How the performances of the Lead ISEs were affected in changing the current density during the electrodeposition of PEDOT
● Standard deviation for the baseline of the ISEs
■ Standard deviation for the sensitivity of the ISEs

## Slide 12
11
GNPs
● Introduction ● Solid Contact Material ● Conclusions ● Future Trends
GNPs used like solid contact for different reasons:
  possibility of tuning in changing the solvent and the ligand for specific applications
  tuned to directly bind the metal ion of interest
  like others nanomaterials, ability to increase the surface area of the sensitive part of the solid contact

## Slide 13
12
GNPs
● Introduction ● Solid Contact Material ● Conclusions ● Future Trends
Thioctic Acid GNPs Thioctic Amide GNPs
soluble in water
functionalization by ligand exchange
dmean = 3.6 ± 0.6 nm
soluble in DMSO
functionalization by ligand exchange
dmean = 3.5 ± 0.7 nm
Notes: checking the size distribution

## Slide 14
13
GNPs
● Introduction ● Solid Contact Material ● Conclusions ● Future Trends
Thioctic Acid GNPs
10 monolayers
SENSITIVITY: 26.68 mV
LOD: 6.87
50 monolayers
SENSITIVITY: 31.91 mV
LOD: 6.53
Notes: checking the size distribution

## Slide 15
14
GNPs
● Introduction ● Solid Contact Material ● Conclusions ● Future Trends
Thioctic Amide GNPs
10 monolayers
SENSITIVITY: 33.93 mV
LOD: 7.2
50 monolayers
SENSITIVITY: 26.36 mV
LOD: 7.9
Notes: checking the size distribution

## Slide 16
15
Conclusions
● Introduction ● Solid Contact Materials ● Conclusions ● Future Trends
  The study of optimization for screen printed electrodes using different materials for the solid contact showed:
    POT: dependence from the thickness of the conducting polymer
    PEDOT: dependence from the thickness and the redox state of the conducting polymer
.
    GNPs were used for the first time like solid contact on top of screen printed electrodes and tuning the ligand
Improvements into the LOD

## Slide 17
16
Future Trends
● Introduction ● POT ● PEDOT ● GNPs ● Conclusions ● Future Trends
.
Need for an optimization of the other key layer
MEMBRANE
Optimization into the use of GNPs (best ligand, solvent) to have to exploit all their different properties
Creation of calibrationless sensors directly integrated into wireless platforms for environmental/wearable applications .

## Slide 18
Acknowledgements
Dr. Claudio Zuliani
Prof. Dermot Diamond
All the people in room N205 and SG03
We would like to acknowledge Science Foundation Ireland - 07/CE/I1147 – supporting "CLARITY: Centre for Sensor Web Technologies"
17