## Slide 1: Thermo-responsive Poly(Ionic Liquid) Valves for Microfluidic Devices
Alexandru Tudor, Janire Saez, Larisa Florea, Fernando Benito-Lopez and Dermot Diamond

## Slide 2: The Origin of Ionic Liquids
Paul Walden (1863-1957)
1914
Ethylammonium Nitrate

## Slide 3: Ionic Liquids
Common cations
Common anions
-
+

## Slide 4: Ionic Liquid Monomers
Cationic
Anionic
+
-

## Slide 5
Tributylhexyl Phosphonium Sulfopropyl Acrylate (P4446-SPA)
Crosslinked Poly(Ionic liquid)s
Polypropylene Glycol Diacrylate
Crosslinker
Monomer

## Slide 6: Poly (Ionic Liquid) Hydrogels
P4446-SPA
Photoinitiator
H2O + Acetonitrile
5 %m Crosslinker
3 mm
1 mm
~200 kLux for 30min
1 mm

## Slide 7
Chart: Time (minutes)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24
 | 14.1959 | 13.3555 | 12.9886 | 12.7079 | 12.4077 | 12.2589 | 12.1454 | 12.1339 | 12.633 | 13.9039 | 14.3412 | 14.7692 | 14.9388 | 15.1929 | 15.4843 | 15.7329 | 15.0384 | 14.1699 | 13.5221 | 13.3916 | 13.1391 | 12.8819 | 12.5831 | 12.3306
1% w/w NaCl
1% w/w NaCl
DI Water
1 mm

## Slide 8: Temperature Responsive Poly(Ionic Liquid)s
+
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+

## Slide 9
Chart: Time (min)
| 0 | 8 | 16 | 24 | 32 | 40 | 48 | 56 | 64 | 72 | 80 | 88 | 96 | 104 | 112 | 120 | 128 | 136 | 144 | 152 | 160 | 168 | 176 | 184 | 192 | 200 | 208 | 216 | 224 | 232 | 240
 | 13.8913 | 13.5816 | 12.8376 | 11.9991 | 10.3184 | 9.4206 | 8.4812 | 8.0615 | 7.2786 | 6.6247 | 6.0567 | 6.0773 | 6.0864 | 6.0895 | 6.1374 | 6.9807 | 8.777 | 10.9836 | 12.7293 | 12.9372 | 14.2313 | 13.5601 | 13.0266 | 11.8187 | 10.5841 | 8.5368 | 7.1866 | 6.6672 | 6.3874 | 6.1913 | 6.0264
 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 65 | 60 | 55 | 50 | 45 | 40 | 35 | 30 | 25 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70
Heating
Cooling
Heating
1 mm

## Slide 10: Swelling-Reswelling Cycle
Chart: Time (min)
| 0 | 8 | 16 | 24 | 32 | 40 | 48 | 56 | 64 | 72 | 80 | 88
Total Average (mm²) | 14.5332 | 8.1353 | 13.7062 | 7.9991 | 14.3394 | 7.8317 | 13.979 | 7.7922 | 13.9724 | 8.2239 | 14.095 | 8.0451
Total Average (mm²) | 14.5332 | 8.1353 | 13.7062 | 7.9991 | 14.3394 | 7.8317 | 13.979 | 7.7922 | 13.9724 | 8.2239 | 14.095 | 8.0451
20 oC
50 oC

## Slide 11: Microfluidic Chip Fabrication
Inlet
Outlet
Gel Chamber
Channel
Top view
Gel Chamber
Gel Chamber
From
20 oC to 50 oC
Side view
Channel
Channel
Syringe Pump
Chip
Heater
Nanoflow meter
500 nL·min-1
20 oC to 50 oC
20 oC to 50 oC

## Slide 12: Temperature-regulated Flow
Chart: Time (s)
50 °C
20 °C

## Slide 13: Shrinking and Swelling Kinetics
Chart: Time (s)
Chart: Time (s)

## Slide 14: Acknowledgements
Dr. Larisa Florea, Dr. Simon Gallagher, Dr. Simon Coleman.
Dr. Fernando Benito-Lopez, Janire Saez.
Conor O’Quigley, Tom Glennon.
Wayne Francis, Aishling Dunne, Danielle Bruen, Jennifer Deignan.
John Burns, Joseph Hennesy.
Prof. Dermot Diamond.
Marie Curie ITN FP7 OrgBIO project.

## Slide 15: Conclusions
Thermo-responsive P4446-SPA hydrogels can be used as temperature-operated valves in microfluidic devices.
Further investigate the possibilities of using the P4446-SPA hydrogels as flow regulators in microfluidic chips.

## Slide 16
Valve shrinking kinetics
Where:
the maximum value of the curve
the intercept
the slope
the offset

## Slide 17: Rate constant calculation results
Shrinking |  |  | Swelling | 
Repetition | C |  | Repetition | C
1 | 0,89 |  | 1 | 0,91
2 | 0,36 |  | 2 | 0,94
3 | 0,52 |  | 3 | 0,83
4 | 0,80 |  | 4 | 0,38
5 | 0,67 |  | 5 | 0,49
6 | 0,62 |  | 6 | 
MEAN | 0,64 |  | MEAN | 0,71
DESVEST | 0,19 |  | DESVEST | 0,26
RSD (%) | 29,80 |  | RSD (%) | 36,41

## Slide 18
1 mm

## Slide 19: Salt Concentration Induced Shrinking
Chart: Time (minutes)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24
 | 14.1959 | 13.3555 | 12.9886 | 12.7079 | 12.4077 | 12.2589 | 12.1454 | 12.1339 | 12.633 | 13.9039 | 14.3412 | 14.7692 | 14.9388 | 15.1929 | 15.4843 | 15.7329 | 15.0384 | 14.1699 | 13.5221 | 13.3916 | 13.1391 | 12.8819 | 12.5831 | 12.3306
1% w/w NaCl
1% w/w NaCl
DI Water

## Slide 20
1 mm

## Slide 21: Temperature-induced Shrinking Kinetics
Chart: Time (min)
| 0 | 8 | 16 | 24 | 32 | 40 | 48 | 56 | 64 | 72 | 80 | 88 | 96 | 104 | 112 | 120 | 128 | 136 | 144 | 152 | 160 | 168 | 176 | 184 | 192 | 200 | 208 | 216 | 224 | 232 | 240
 | 13.8913 | 13.5816 | 12.8376 | 11.9991 | 10.3184 | 9.4206 | 8.4812 | 8.0615 | 7.2786 | 6.6247 | 6.0567 | 6.0773 | 6.0864 | 6.0895 | 6.1374 | 6.9807 | 8.777 | 10.9836 | 12.7293 | 12.9372 | 14.2313 | 13.5601 | 13.0266 | 11.8187 | 10.5841 | 8.5368 | 7.1866 | 6.6672 | 6.3874 | 6.1913 | 6.0264
 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 65 | 60 | 55 | 50 | 45 | 40 | 35 | 30 | 25 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70
Heating
Cooling
Heating

## Slide 22: Valve Shrinking Kinetics
Chart: 3
Chart: 5
Chart: 6
Chart: 4
Chart: 1
Chart: 2

## Slide 23: Valve Swelling Kinetics
Chart: 2
Chart: 3
Chart: 4
Chart: 5
Chart: 1