## Slide 1: Thermo-responsive Poly(Ionic Liquid) Hydrogel Microfluidic Valves
Alexandru Tudor, Janire Saez, Larisa Florea, Fernando Benito-Lopez and Dermot Diamond

## Slide 2
Tributylhexyl Phosphonium Sulfopropyl Acrylate (P4446-SPA)
Crosslinked Poly(Ionic liquid)s
Polypropylene Glycol Diacrylate
Crosslinker
Monomer

## Slide 3: Poly (Ionic Liquid) Hydrogels
P4446-SPA
Photoinitiator
H2O + Acetonitrile
5 %m Crosslinker
3 mm
1 mm
~200 kLux for 30min
1 mm

## Slide 4
Chart: Time (min)
| 0 | 8 | 16 | 24 | 32 | 40 | 48 | 56 | 64 | 72 | 80 | 88 | 96 | 104 | 112 | 120 | 128 | 136 | 144 | 152 | 160 | 168 | 176 | 184 | 192 | 200 | 208 | 216 | 224 | 232 | 240
 | 13.8913 | 13.5816 | 12.8376 | 11.9991 | 10.3184 | 9.4206 | 8.4812 | 8.0615 | 7.2786 | 6.6247 | 6.0567 | 6.0773 | 6.0864 | 6.0895 | 6.1374 | 6.9807 | 8.777 | 10.9836 | 12.7293 | 12.9372 | 14.2313 | 13.5601 | 13.0266 | 11.8187 | 10.5841 | 8.5368 | 7.1866 | 6.6672 | 6.3874 | 6.1913 | 6.0264
 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 65 | 60 | 55 | 50 | 45 | 40 | 35 | 30 | 25 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70
Heating
Cooling
Heating
1 mm

## Slide 5: Microfluidic Chip Fabrication
Inlet
Outlet
Gel Chamber
Channel
Top view
Gel Chamber
Gel Chamber
From
20 oC to 50 oC
Side view
Channel
Channel
Syringe Pump
Chip
Heater
Nanoflow meter
500 nL·min-1
20 oC to 50 oC
20 oC to 50 oC

## Slide 6: Temperature-regulated Flow
Chart: Time (s)
50 °C
20 °C

## Slide 7: Shrinking and Swelling Kinetics
Chart: Time (s)
Chart: Time (s)

## Slide 8: Acknowledgements
Dr. Larisa Florea, Dr. Simon Gallagher, Dr. Simon Coleman.
Dr. Fernando Benito-Lopez, Janire Saez.
Conor O’Quigley, Tom Glennon.
Wayne Francis, Aishling Dunne, Danielle Bruen, Jennifer Deignan.
John Burns, Joseph Hennesy.
Prof. Dermot Diamond.
Marie Curie ITN FP7 OrgBIO project.