## Slide 1: Solvent Sensing Fluorescent poly(Ionic Liquid) Ionogels
Alexandru Tudor, Adam McColgan, Colm Delany, Larisa Florea, Dermot Diamond

## Slide 2: The Origin of Ionic Liquids
Paul Walden (1863-1957)
1914
Ethylammonium Nitrate
1-methyl-3-ethyl imidazolium
1992

## Slide 3: Ionic Liquids
Common cations
Common anions
-
+

## Slide 4: Fluorescein

## Slide 5: Acid-Base Equilibrium of Fluorescein

## Slide 6: Fluorescein-based Ionic Liquid
Trihexyltetradecyl Phosphonium Fluorescein

## Slide 7: Ionic Liquid Monomers
Cationic
Anionic
+
-

## Slide 8
Tetrabutyl Phosphonium Sulfopropyl Methacrylate (P4444-SPMA)
Crosslinked Poly(Ionic liquid)s Ionogels
Polypropylene Glycol Diacrylate
Crosslinker
Monomer
Ionic Liquid
Trihexyltetradecyl Phosphonium Fluorescein

## Slide 9: Poly (Ionic Liquid) Fluorescent Ionogels
P4444-SPMA
Photoinitiator
H2O + Methanol
5 %m Crosslinker
3 mm
1 mm
for 30min
3.5 mW·cm-2

## Slide 10: Poly(Ionic Liquid)s
+
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
PFl
PFl
PFl

## Slide 11: Ionogel Swelling
Hexane
Toluene
Acetone
Acetonitrile
Dichloromethane
Methanol

## Slide 12: Fluorescence Spectroscopy
Chart: Wavelength (nm)

## Slide 13: Fluorescence Spectroscopy
Chart: Wavelength (nm)

## Slide 14: Conclusions
Future Work
A fluorescein ionic liquid was synthesized
A solvatochromic ionogel was synthesised and it had its solvent response characterized
Synthesise ionogels containing different dissolved functional organic compounds and ionic liquids such as boronic acid derivatives for glucose sensing
  Enlarge the ionic liquid and ionic liquid monomer toolbox

## Slide 15: Acknowledgements
Dr. Larisa Florea, Dr. Simon Gallagher, Dr. Simon Coleman, Dr. Colm Delaney.
Conor O’Quigley, Tom Glennon.
Wayne Francis, Aishling Dunne, Danielle Bruen, Jennifer Deignan.
Adam McColgan.
Prof. Dermot Diamond.
Marie Curie ITN FP7 OrgBIO project.

## Slide 16: UV-Vis Spectrophotometry
Chart: Wavelength (nm)

## Slide 17: UV-Vis Spectrophotometry
Chart: Wavelength (nm)

## Slide 18: Fluorescence Spectroscopy
Chart: Wavelength (nm)

## Slide 19: Fluorescence Spectroscopy
Chart: Wavelength (nm)